# Additive Manufacturing and Repair

# Lew Kindleyside and Wesley Cantwell

| Principal Investigator: Name and Contact Details Date: | Approved by Director of ARIC: Name Date: |
| --- | --- |
| Approved by: ARIC Senior Management Board Date of meeting: |  |

# Project definition

This project will investigate the potential offered by additive manufacturing (AM) techniques for repairing damaged components and manufacturing high-performance load-bearing structures for use across a range of industrial sectors. The research activities within this project will be based around the EOS 400-4 metal printer, although other printers, such as the BigRep will be used as and when needed. Attention will focus on manufacturing and repairing components to levels that satisfied industrial norms. Research will focus on the possibility of using AM to repair damaged or degraded aerospace components, such as those found in an aircraft engine. A second area of research activity will seek to develop and demonstrate the benefits of using AM to develop solution for healthcare and broader industrial applications.

# Objectives

-          Repair of aerospace components using additive manufacturing techniques

-          Develop and demonstrate additive manufacturing on new applications for healthcare and industrial applications.

# Approach

Repair of aerospace components

This activity will demonstrate the feasibility of repairing damaged tools, fixtures and components using additive manufacturing, focusing on laser-powder bed fusion. Attention will focus on components that are otherwise challenging and not cost effective using traditional repair methods.

Advantages of laser-powder bed fusion (L-PBF)

•Repairing multiple parts simultaneously

•Complex parts with tight tolerances

•Reduction in post-processing

The ability to successfully melt onto traditionally manufactured components is crucial to using L-PBF as a method of repair. Previous research has shown that it is possible to create an interface between a traditionally-manufactured part and a sintered material using similar metals, ensuring component failure is predictable and not at the interface. Interface parameters could be crucial to creating a strong bond.

Challenges

Positioning the part in the machine is a crucial step in the method for repair. Multiple aspects need to be considered, such as component height and alignment to the CAD/laser. Siemens offer a method for overcoming this by using bespoke software to correctly align within the machine. Extremely high accuracy is required. Multiple parts need to be around 10/20 microns of each other in height. The general method of meeting this was to place parts in fixture then CNC mill and then place the fixture in LPBF machine.

Material Properties

Areas of Focus;

Material Properties at the Joint

An in-depth study will be conducted that will identify the material properties where the additively-manufactured material is melted to the existing component and how it performs. Here, a fracture mechanics-type specimen, such as a single edge notch bend (SENB) sample will be used. Here, a thick flat plate (the part to be repaired) will be installed in the EOS400-4 and builds will be completed on it. The boundary between the original plate and the new build will effectively become the joint. SENB samples will then be prepared in which the joint is located at the mid-point of the specimen. A pre-crack will be introduced at this location and a fracture mechanics test conducted. This approach will yield a fundamental understanding of the fracture properties of the joint between the ‘new’ and ‘old’ material and will be used to identify the optimum parameters for structural repair.

Repaired substrate

New build

Samples removed from build

SENB sample with pre-crack

The approach will be used to identify the effect of varying key parameters on the strength of the repair, including:

Laser power

Scanning speed

Layer thickness

Component Repair

Areas of Focus

Machining of Damaged Components/ Tools

It is critically important that the region that is to be repaired has a flatness within 10 microns relative to the powder bed.

Fixturing

Fixturing and positioning are extremely important issues in terms of achieving a successful repair. Here, an accurate locating/positioning system will be developed that will accurately locate and secure the component within the system build chamber, resulting in the precise deposition of material in the critical region. A study will be undertaken to investigate positioning of the sample wherein parts will be installed, processed using L-PBF, removed and then the cycle will be repeated a number of times in order to investigate alignment of the various builds.

Component Repair

Following discussion with key stakeholders an appropriate component for repair will be identified. The component will be machined (if necessary) and repaired using the L-PBF approach.

Multiple Component Repair

The process will be advanced so that it is capable of repairing several components simultaneously by optimizing the component machining and fixturing processes.

# Expected deliverables

- Deliver to industry a repeatable and reliable method for using L-PBF to repair damage components. (October 2021)

- A demonstrator/prototype highlighting the potential of L-PBF in repairing damaged parts. (September 2021)

- A journal paper that documents the feasibility of using L-PBF to repair damaged or degraded components. (December 2021).

# Human Resources

Lewis Kindleyside (60%)

# Gantt Chart or Timeline

Repair project

# Estimated budget inc. all costs, such as manpower, OPEX and CAPEX.

Consumables – AED 150,000

8 	    Equipment requirements

EOS 400-4

Shot peening equipment

CNC bandsaw

Milling, Turning, CNC

X-CT scanner

Mechanical testing equipment

BigRep polymer printer

9.	    Project specific SMART KPIs

Two UAE Nationals involved on projects

Two journal papers in Q1 journals.

10. 	   Progress reporting requirements

Monthly reports

Updates at the monthly meetings