# Graphene-based Sensors for Composites Monitoring

# M. Alkrunz and Wesley Cantwell

| Principal Investigator: Wesley Cantwell Date: December 2021 | Approved by Director of ARIC: Wesley Cantwell Date: |
| --- | --- |
| Approved by: ARIC Senior Management Board Date of meeting: |  |

# Project definition

Graphene-coated glass fiber tows will be used to monitor strain and detect damage in composite materials based on glass and carbon fiber reinforced epoxy resin. The graphene sensors will be located at different locations within the thickness of the composite and monitored whilst the panels are being subjected to out-of-plane loading by a hemispherical indentor. Initial tests on a glass fiber reinforced epoxy composite have already shown that the sensors are capable of detecting strain as the plate is loaded transversely and ultimately they can detect the onset of damage associated with the onset of fiber fracture and localized delamination. This will be explored further herein. Cyclic fatigue tests highlighting the repeatability of the sensors as well as their ability to withstand longer term loading will also be undertaken. Tests will also be undertaken on carbon fiber reinforced epoxy panels, where it will be necessary to electrically-insulate the sensors from the conductive carbon fibers.

# Objectives

-          To investigate the possibility of using graphene-coated tows for sensing strain in composite materials.

-          To investigate the effect of repeated loading on the strain-sensing capability of graphene-coated tows.

# Approach

Graphene oxide (GO) is an important derivative of graphene, which is rich in oxygen-containing groups on the surface and edges of the graphene-based sheets and prepared from graphite by oxidation reaction. GO can be prepared by oxidizing graphite with a strong oxidant in a concentrated acid. Here in, aqueous GO HCL-free 25% paste supplied will be dissolved in distilled water for the preparation of the GO solution to be used as a coating for the dry fibers.

The dry tows will be taken from a woven glass fabric. The coating process will be started by dissolving graphene oxide paste in distilled water to form a solution (2 g/100 ml). The graphite oxide solution will then be subjected to ultrasonication to exfoliate GO. The tows of the dry glass fabric will be soaked in the solution overnight and then dried in a controlled environment at 180C for 8 hours to reduce the graphene oxide to enhance the conductivity. This approach has worked previously. After coating the tows will be embedded in between the layers of a curing epoxy glass fiber, Figure 1.

The research will be defined through a group of indentation experiments to indentify the resistive response at a specific loading either directly above the sensors or near them at a fixed distance. The testing will focus on studying the combination of mechanical and electrical testing at the same stage. An Instron 5399 will be used to apply the compression load, different loads will be applied by a metallic rod with a spherical end indentor. Two compression loading approaches will be applied, step loading and cyclic loading to study the difference in resistivity while the load is applied.

Wire

Copper tape

Graphene sensor

Glass fiber epoxy layer

Figure 1. Schematic diagram showing the embedded sensors.

The findings of this work will feed into the RIC-2D proposal.

# Expected deliverables

- Representative demonstrator

- One journal paper in Q1 journal.

- Basic information for RIC-2D proposal.

# Human Resources

M. Alkrunz (100%)

# Gantt Chart or Timeline

| Work Package | Month |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12 |
| Literature study |  |  |  |  |  |  |  |  |  |  |  |  |
| Initial tests on sensors - tension |  |  |  |  |  |  |  |  |  |  |  |  |
| Manufacture of composite panels |  |  |  |  |  |  |  |  |  |  |  |  |
| Indentation tests on panels |  |  |  |  |  |  |  |  |  |  |  |  |
| Damage investigation following testing |  |  |  |  |  |  |  |  |  |  |  |  |
| Preparation of Publication |  |  |  |  |  |  |  |  |  |  |  |  |

# Estimated budget inc. all costs, such as manpower, OPEX and CAPEX.

Consumables – All materials are currently available at KU. No new equipment required.

8 	    Equipment requirements

Graphene coating equipment in Composites Laboratory

Small Instron testing machine

Data logging machine

Scanning electron microscope

9.	    Project specific SMART KPIs

Representative demonstrator

One journal paper in Q1 journals.

10. 	   Progress reporting requirements

Monthly reports

Updates at the monthly meetings